Structural Effect of Low-dimensional Carbon Nanostructures on Long-term Stability of Dye Sensitized Solar Cells

Rusoma Akilimalia, Gurpreet Singh Selopala,b *, Mahyar Mohammadnezhada, Ibrahima Kaa, Zhiming M. Wang,b, d,  Gregory P. Lopinskic, Haiguang Zhao e, Federico Roseia,b*

a Institut National de la Recherche Scientifique, Centre Énergie, Matériaux et Télécommunications, 1650 Boul. Lionel Boulet Varennes, Québec, J3X 1P7, Canada.

b Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu, Sichuan 610054, P. R. China.

c Metrology Research Center, National Research Council Canada, 100 Sussex Dr., Ottawa, ON, K1A 0R6, Canada.

dInstitute for Advanced Study, Chengdu University, Chengdu, Sichuan 610106, P.R. China.

e State Key Laboratory of Bio-Fibers and Eco-Textiles, Qingdao University, No. 308 Ningxia Road, Qingdao 266071, P. R. China.

Email: gurpreet.selopal@inrs.ca; federico.rosei@inrs.ca

Figure 1S. Schematic of DSSCs components with TiO2, FLG-TiO2 and GNR-TiO2 hybrid photoanodes highlighting preferred electrons transport through FLG and GNR within mesoporous film toward FTO.

Table 1S. Structural parameters of as received GNR and FLG.

| Parameters | No. of Atomic Layers (n) | Width (d) | Length (l) |
| --- | --- | --- | --- |
| GNRs | 1 | 100-180 nm | 2-15 μm |
| FLG | 5-7 | 200-250 nm | 2-6 μm |

Figure 2S (a) UV-Vis absorption of TiO2, TiO2 with FLG and GNR hybrid photoanodes. (b) Absorption spectra of dye removal solution. (c) Dye loading vs photoanode structure.

Figure 3S (a) IPCE curve for DSSCs device based on TiO2, TiO2 with FLG and GNR hybrid photoanodes; (b) Integrated Jsc curves obtained from IPCE curves for the corresponding devices.

Figure 4S. Electrochemical impedance spectroscopy (EIS) analysis of DSSCs based on TiO2, Graphene-TiO2 and GNR-TiO2 hybrid photoanodes before (lighter color) and after 270h (darker colours) simulated sun exposure under dark measurement: (a) chemical capacitance Cμ; (b) chemical capacitance variations dCμ

Figure 5S. Histograms of evolution of the percentage change between Graphene and GNR, before and after light soaking for Rct (a), τn (b) and Cμ (c). Evolution of τn as of Cμ before and after light soaking for Bare sample (d), Graphene (e) and GNR based sample (f)